## Slide 1: MURI Update
Aaron Holsteen & Mark Brongersma
September 14, 2015

## Slide 2
Tunability of Optical Resonances in High Index Nanostructures
Size
Polarization
Cao, Brongersma et al., Nano Lett., 2649–2654, 10, 2010.
Cao, Brongersma et al., Nano Lett., 10, 439–445 (2010).
30 nm
180 nm
130 nm
Shape
Coupling
50nm
Example: Resonances of Si nanowires and beams

## Slide 3
Optical Properties of Dielectric/Semiconductor Structures
 For top-illumination resonances split in TM and TE modes
|H|2
TE01
TE11
TM11
TM01
 For 100 nm wide rectangular nanowires, the two lowest order resonances apparent in the visible
Notes: M = number of wavelength around the circumference; L is radial order

## Slide 4
m = αMH
Dipolar nature of TE01 and TE11 modes above a mirror
p = αEE
Point Dipole Model
Explore mechanisms to make tunable metasurface devices utilizing these resonances
Tuning Across the Visible
Spectrum
Understand why these dipolar-like resonances respond the way they do near a mirror
Project Goals:

## Slide 5
Measuring optical scattering of nanowires
SiNW
Dark Field Image
Scattering Spectra
Confocal microscopy and dark field illumination:
Confocal Pinhole
I (a.u.)
Source
Measurement
Mirror
Notes: Now that I have explained the nature of the optical modes supported in Si NWs, let me describe the experimental approach to examine the optical properties of these structures.
Deposit nanostructure: VLS, sonication, and casting or EBL and RIE fabrication
Optical DF imaging
Confocal optical spectrometry via a diffraction grating and areal ccd
Measure the Scattering Cross-section

## Slide 6
TE
TM
Without Mirror
Nanowire Size:
W = 80 nm , H = 105 nm
20 μm
New approach to examine the modulation of excited optical
resonances from long silicon nanowires:
With Mirror
Both polarizations exhibit resonances that are tunable across the visible spectrum
with changes of the height above a mirror.

## Slide 7
Scattering Spectra Without Mirror
Experimental spectral results for the TE Polarization
TE01
TE11
Two resonances are clearly visible as the nanowire gets further away from the mirror, the Mie-like resonances
Fast modulations with height ~100-200 nm present
Slow envelope modulations ~1000 nm present
Optical
Image

## Slide 8
Incident Field
Total Field
Predicting the height variations in the scattered light intensity
Standing Field Above Mirror
NW
p
ηext ~ (Einc)2
Efficiency
NW
ηcol ~ (Escat)2
ηtot ~ ηcol * ηext
Scattered Field

## Slide 9
Separate Excitation of TE01 and TE11 Modes above a mirror
TE01
TE11

## Slide 10: Concluding Remarks
Similar results exist for the TM polarization, with broadband tunability
Next Steps are to look at ways to mechanically control the height to enable active metasurface devices

## Slide 11
Comparison of Experimental and Simulated Light Scattering,
TE Polarization

## Slide 12
Comparison of Experimental and Simulated Light Scattering,
TM Polarization
12