## Slide 1: High Efficiency Mid-Infrared Flat Lenses Based on Reflectarrays and MEMS Scanning Devices
MURI Update on September 16, 2015
Shuyan Zhang,
F. Aieta, I. Gabay, A. She, T. Mansuripur, R. Khorasaninejad, D. Rousso, F. Capasso
(Harvard University)
M. H. Kim and N. Yu
(Columbia University)
R. Tapashree, I. W. Jung, D. Lopez
(Argonne National Laboratory)

## Slide 2: Our Goal
Design & fabricate a flat lens in the mid-ir (4.6 μm):
  High focusing efficiency
  Simple fabrication steps
  Polarization independent
  CMOS compatible: large scale applications
  MEMS based SLMs

## Slide 3: Design & Fabrication
Design parameters:
D=3.08 mm (size of lens, 1233 antennas)
=45o (beaming angle), h=400 nm
r=4 cm (focal distance)
Reflection mode:
Focusing into a line at an angle like cylindrical lens
Future: demonstration of spherical lens functionality
Fabrication techniques:
E-beam evaporation, PECVD, deep-UV lithography
Materials: Au and SiO2
Design principles:

## Slide 4: Experimental Setup
Source
Fabry-Perot QCL 4.6 μm
Lens
Multiple lenses on a 6-inch wafer
Signal collection
Lock-in amplifier PC
Scanning
Motorized rotational & translational stages
Detector
TE-cooled detector 50 µm pinhole

## Slide 5: Experiment vs Simulation
Angle scan:
X’ Scan:
Full beam waist @ 1/e2 = 185 μm

## Slide 6: Conclusion
Summary of features
  Metasurface based flat lens that focuses ir light from 3 mm beam waist down to 185 μm beam waist
  The measured focusing efficiency is 72% and the simulated efficiency is 80%.
Outlook
  Applications in ir imaging, detection, and focused beam steering
  MEMS scanners integrated with flat optics for compact imaging/scanning probes: collaboration with D. Lopez Group at Argonne National Lab (world leader in MEMS Technology)

## Slide 7
Slide adapted from Il Woong Jung (Argonne National Laboratory)
Lens on membrane

## Slide 8
Nano-welding of flat lens on MEMS
bare MEMS
900 μm
weldings
probe
MEMS with lens
MEMS with lens
Slide adapted from Roy Tapashree
(Argonne National Laboratory)

## Slide 9
Slide adapted from Il Woong Jung (Argonne National Laboratory)

## Slide 10: appendix

## Slide 11
1190 um
1190 um
800 um
Backside
Frontside
Making a flat lens membrane
Frontside
after etch
Mag 100 x
NA 0.9
Au 50 nm
SiO2 400 nm
Au 200 nm
Silicon 2000 nm
SiO2 200 nm
Silicon 600000 nm
SiO2 110 nm
membrane 2.85 um
XeF2