## Slide 1
Metasurfaces from
Bulk Diamond
Haig Atikian, Xiao Xiong & Marko Loncar
Laboratory for Nanoscale Optics
Loncar Group
School of Engineering and Applied Sciences, Harvard University
9 Oxford Street, Cambridge, MA 02138

## Slide 2: Laser Damage Threshold
Laser light can have very high optical intensities
Therefore, laser light often causes laser-induced damage of optical components like mirrors, lens, polarizers. etc.
For various applications, one needs to select optical components with a sufficiently high optical damage threshold (LIDT).
http://www.zmescience.com/science/physics/high-power-laser-hallow-atom-inside-out-0432423/
http://techno-comps.blogspot.com/2011/04/top-five-future-weapons.html

## Slide 3: Laser Damage Threshold
Optical damage can arise within a bulk piece of optical material, but also on its surfaces
Surfaces often exhibit a higher density of microscopic defects than bulk material, typically being the site of laser damage.
Damage threshold can depend on the bulk material, as well as surface layers, which could substantially lower the LIDT compared to the bulk.
Power handling capabilities could be improved using bulk substrates with excellent thermal and optical properties (diamond)
https://www.rp-photonics.com/laser_induced_damage.html

## Slide 4: Diamond’s Appeal
Chemically inert
Biologically compatible
Surface functionalization possible
Widest bandgap (~5.5eV)
Low dielectric loss
Both n- and p-type doping
Wide transmission window
Large refractive index (2.4)
Highest thermal conductivity
Low thermal expansion
Diamond
Mechanical
Thermal
Optical
Biological
Chemical
Electrical
…engineer’s best friend
Hardest material
Low mass density
High Young’s modulus

## Slide 5: Nanostructure diamond surface
5
h_total
r_disc
r_min
r_sup
alpha
Nanostructure the diamond surface with a structure that has varying diameter width along the vertical direction, to create a metasurface effect from the bulk diamond

## Slide 6: FDTD Simulations Perfect Reflection
6
h_total=3um
r_min=0.04um
r_sup=0.2um
pitch=1um
～50nm
r_disc = 0.4um
h_total
r_disc
r_min
r_sup
alpha

## Slide 7: FDTD Simulations Perfect Reflection
7
Sweep Pitch
Sweep r_disc
Sweep h_total

## Slide 8: Device fabrication

## Slide 9: Device fabrication

## Slide 10: Device fabrication

## Slide 11: Summary and Outlook
Summary
Fabrication technique improvement to create larger area diamond metasurfaces
Flexible design parameters for tuning bandwidth and operation wavelength
Outlook
Measure experimental results with high intensity lasers to ensure high power handling capabilities