## Slide 1: Lithium Niobate (LN) Metasurface for Second Harmonic Generation -Fabrication summary
MURI Conference Call 09/16/15
Cheng Wang, Marko Lončar Harvard University
Zhaoyi Li, Nanfang Yu Columbia Unviersity

## Slide 2: LN Fabrication Capability
Previous fabrication of high quality LN nanostructures
Highest measured Q in microdisk ~ 100,000
Fab method applicable for rings, waveguides, etc.
[1] C. Wang et al., Integrated high quality factor lithium niobate microdisk resonators, Opt. Express (2014).

## Slide 3: Fabrication Procedure
LN
LN
SiO2
FOX-16
Spin FOX-16 on LNOI substrate (400 nm LN)
LN
LN
SiO2
FOX-16
E-beam Lithography
LN
SiO2
RIE w/ Ar+ to form an LN ridge waveguide (300 nm etching depth)
FOX-16
LN ridge waveguides
LN
LN
SiO2
Remove residue FOX-16 and PECVD 75 nm of amorphous Si
LN
LN
SiO2
Spin on diluted FOX-16 (1:1 with MIBK)
FOX-16
LN
SiO2
LN ridge waveguides
a-Si antenna
E-beam Lithography with Alignment; RIE to form a-Si antenna

## Slide 4: a-Si antennae on top of LN waveguides
Initial test done on bulk LN samples
Left: resist defined by e-beam lithography with alignment
Right: Si antennae after removing resist
Notes: Slightly misaligned; overetched

## Slide 5: Future Plan
Fabrication of Si-LN antenna arrays on x-cut LN thin films
Device characterization:
  Butt-coupling with lensed fibers
  Pump with tunable CW telecom laser (1480 – 1680 nm, max power 20 mW)
  SHG light detection using APD
  ~ 100,000 cps with phase mismatched waveguides
  EDFA & OSA available for high power measurements

## Slide 6: Q&A
Thank you!

## Slide 7: µ-disk Transmission Spectrum (Telecom)
Highest measured Q ~ 100,000
in telecom
(a)
17.0 pm
Q ~ 88,000
14.8 pm
Q ~ 102,000
35.3 pm
Q ~ 44,000
(c)
(b)
(d)
(e)
(f)
(g)
TE88, 02
TE87, 02
TE86, 02
TE85, 02
TE94, 01
TE93, 01
TE92, 01
TE82, 03
TE81, 03
TE80, 03
TE88,02 neff = 1.53
TE94,01 neff = 1.63
TE80,03 neff = 1.42
[1] C. Wang et al., Integrated high quality factor lithium niobate microdisk resonators, Opt. Express (2014).
Notes: TM modes are not supported in telecom wavelengths since the film is too thin

## Slide 8: Integrated LN Photonic Platform
Loaded Q ~ 25,000
Close to critical coupling
Intrinsic Qint ~ 50,000
Q = 25,000
Highest measured Q on integrated LN platform
~ 65,000

## Slide 9: Integrated LN Photonic Platform
Sample under test
Lensed fiber
Tunable Laser
Fiber polarization controller
Photodetector
(APD)