## Slide 1: Harvard- MURI Meeting September 16, 2015
Prof. Vladimir Shalaev
Prof. Alexandra Boltasseva
Prof. Alexander Kildishev

## Slide 2: Short Updates
Accepted for Optica:
Amr Shaltout, Jingjing Liu, Alexander Kildishev, Vladimir Shalaev, “Photonic Spin Hall Effect Photonic Spin Hall Effect in Gap-Plasmon Metasurfaces for On-Chip Chiroptical Spectroscopy”, Optica 2(9), 2015
Submitted:
Amr Shaltout, Alexander Kildishev, Vladimir Shalaev, “Time-Varying Metasurfaces and Lorentz Non-Reciprocity”, submitted for Optical Materials Express, plasmonics Issue
CD Spectrometer
Time-Varying Metasurfaces
Ultrafast Laser Beam Steering
CD Spectrometer
Time-Varying Metasurfaces
Ultrafast Laser Beam Steering
Metasurfaces feeded by spectral components of ultrashort pulses
τ ~ 100 ps
Theory and simulation completed
Experimentation in progress

## Slide 3: ZrN Metasurfaces
Krishnakali Chaudhuri
Amr Shaltout
Prof. Vladimir Shalaev
Prof. Alexandra Boltasseva

## Slide 4: ZrN Metasurface
Replication of already existing phenomena: Photonic Spin Hall effect
PSHE application example : Circular Dichroism Spectrometer*, and all Berry phase based applications.
rx, ry : complex coefficients of reflection of a single nano antenna in x- and y- direction
For RCP wave incidence:
For LCP wave incidence :
Theory:
*Ref: Shaltout et al, “Photonic Spin Hall Effect in Gap-Plasmon Metasurfaces for On-Chip Chiroptical Spectroscopy” submitted (Shalaev Group)

## Slide 5: Optimized design of rectangular antenna with ZrN
Px | 250[nm]
Py | 250[nm]
t_sup | 650[nm]
t_mirror | 100[nm]
t_spacer | 50[nm]
t_antenna | 80[nm]
ep_sup | 1
ep_spacer | 4.82
hmax | 50[nm]
t_Si | 500[nm]
W1 | 110[nm]
W2 | 180[nm]
Fabrication issue: Dry etching
  Cl2/Ar : Slower etch rate, longer etch duration, compromised selectivity with resist
  BCl3: Very high etch rate, Controlled etching- Experiments ongoing
Extendable into other applications of phase gradient metasurface
ZrN
ZrN
AlScN
Substrate
80nm
50nm
100nm
250nm
*Ref: Shaltout et al, “Photonic Spin Hall Effect in Gap-Plasmon Metasurfaces for On-Chip Chiroptical Spectroscopy” Accepted for Optica (Shalaev Group)
With Au
*

## Slide 6: Metasurface saturable absorber mirror using ZrN
ZrN mirror
ZrN antennas
Spacer with Kerr type nonlinearity
Incident pulse
Reflected pulse
Field intensity dependent refractive index (large third order kerr type nonlinearity) of the spacer dielectric
Spacer index change will change the reflectivity of the metasurface (depth of modulation for SAM)
ZrN (refractory) can be pumped with much higher power
Preliminary results of observing the pulse narrowing effect using COMSOL multiphysics.

## Slide 7: Experimental Progress for Color Hologram
Sajid Choudhury, Amr Shaltout, Alexander Kildishev, Vladimir Shalaev, Alexandra Boltasseva

## Slide 8: SEM Image of Patterns created with FIB
- Sample: Ag-40nm Ebeam Evaporated on Fused Silica substrate
- Pattern Written with Focused Ion Beam

## Slide 9: RGB Images for the Hologram Pattern
Experiment
Simulation
Sample illuminated separately with Ar-Kr laser, and Super-K Laser (with help of Nate Kinsey) and pattern observed using CCD Camera.